Supplementary Material

Single crystal diffraction data were collected on an Oxford Diffraction SuperNova Diffractometer equipped with an Atlas CCD-detector at T=220 K, using an Oxford Instruments Cryojet HT cooler. Data collection, cell refinement, and data reduction were carried out using CrysAlisPro [1]. Superflip software [2] was used for structure solution and space-group assignment, and JANA2006 [3] for structure refinement. Figures were generated using VESTA [4]. The absorption correction was done analytically using a multifaceted crystal model [5]. No extinction corrections were necessary. From the total number (23429) of measured intensities, we obtained 6068 unique reflections (reflections related by symmetry are merged together), out of which 2523 reflections are satisfying F2>3σ(F2). The calculated vs. observed structure factors are shown in Fig. S2.

| Table I. Crystal Data |  |
| --- | --- |
| Empirical Formula | IrTe2 |
| Formula weight | 447.4 |
| Crystal system | Triclinic |
| Space Group | P-1 (No. 2) |
| Unit Cell Parameters |  |
| a = 3.9548(2) Å |  = 98.129(5)o |
| b = 6.6542(4) Å |  = 92.571(4) o |
| c = 14.4345(7) Å |  = 107.119(5) o |
| Volume | 357.88(4) Å3 |
| Z | 5 |
| Density (calculated) | 10.3767 g/cm3 |
| Absorption coef. | 65.937 mm-1 |
| F(000) | 905 |
| Crystal Size | 101.6x32.8x17.2 m |
| Max. and Min. transmission factors | 0.027 and 0.348 |
| Absorption correction | Analytical |
| Min. and Max. theta angles | 3.23 and 45.42 |

| Table II. Experimental Data |  |
| --- | --- |
| Temperature | 220K |
| Radiation type | Mo K |
| Wavelength | 0.7107 Å |
| Detector resolution | 10.362 pix./mm. |
| Measurement method |  scans |
| Measured Intensities | 23429 |
| Unique reflections | 6068 [ Rint=0.1105] |
| Strong reflections | 2523 |
| Index ranges | -7 ≤ h ≤ 7 -13 ≤ k ≤ 13 -28 ≤ l ≤ 28 |
| Counting time | 10 s/frame |

| Table III. Refinement Data |  |
| --- | --- |
| Data/parameters | 2523 / 70 |
| Refinement Method | Full-matrix least-squares on F2 |
| R1 / wR2 [2523] | 0.0571 / 0.1083 |
| Goodness-of-fit [2523] | 1.44 |
| R1 / wR2 [6068] | 0.1340 / 0.1386 |
| Goodness-of-fit [6068] | 1.19 |

..

S - Goodness-of-fit

Nref – the number of reflections used in the refinement

Nparam - the number of refined parameters

| Table IV. Anisotropic atomic displacement factors Uij(Å2). |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Atom | U11 | U22` | U33 | U12 | U13 | U23 |
| Ir(1) | 0.0087(3) | 0.0123(3) | 0.0078(3) | 0.0039(2) | 0.00103(19) | 0.0047(2) |
| Ir(2) | 0.00821(19) | 0.0123(2) | 0.00788(18) | 0.00386(15) | 0.00092(14) | 0.00474(14) |
| Ir(3) | 0.0087(2) | 0.0130(2) | 0.00803(19) | 0.00401(16) | 0.00096(14) | 0.00464(15) |
| Te(1) | 0.0085(3) | 0.0127(4) | 0.0104(3) | 0.0037(3) | 0.0008(2) | 0.0049(3) |
| Te(2) | 0.0087(3) | 0.0123(4) | 0.0082(3) | 0.0041(3) | 0.0008(2) | 0.0041(2) |
| Te(3) | 0.0089(3) | 0.0119(3) | 0.0080(3) | 0.0038(3) | 0.0006(2) | 0.0042(2) |
| Te(4) | 0.0089(3) | 0.0127(3) | 0.0087(3) | 0.0038(3) | 0.0008(2) | 0.0043(3) |
| Te(5) | 0.0094(3) | 0.0122(3) | 0.0076(3) | 0.0036(3) | 0.0004(2) | 0.0041(2) |

Figure S1. X-ray diffraction pattern in the (H 0 L) reciprocal plane (high-temperature notation) at T=220 K. The high-temperature a0* and c0* directions are given by the (1,0,0) and (0,0,1) Bragg peaks, respectively. The inset shows the structural modulation peaks with q0=(1/5, 0, 1/5).

Figure S2. Observed vs. calculated structure factors squared, F2 satisfying F2>3σ( F2). Statistical error bars are smaller than the symbol size.

References

[1]. CrysAlisPro, Oxford Diffraction Ltd., Version 1.171.36.21 (release 14-08-2012 CrysAlis171.NET).

[2]. Superflip - a computer program for the solution of crystal structures by charge flipping in arbitrary dimensions; L. Palatinus, G. J. Chapuis, Appl. Cryst. 40, 786-790 (2007).

[3]. Jana2006 - Structure Determination Software Programs (Institute of Physics, Prague, Czech Republic) V. Petricek , M. Dusek and L. Palatinus (2006).

[4]. VESTA – a computer program for three-dimensional visualization of crystal, volumetric and morphology data; K. Momma and F. Izumi, J. Appl. Crystallogr. 44, 1272-1276 (2011).

[5]. Analytical numeric absorption correction using a multifaceted crystal model based on expressions derived by R.C. Clark and J.S. Reid; R.C. Clark and J.S. Reid, Acta Cryst. A51, 887-897 (1995).